## Slide 1: Prints 1
Layer height (mm) | 0.1
Print speed (mm/s) | 30
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.394
2 |  | 0.9 mm | 0.334
3 |  | 1.0 mm | 0.308
4 |  | 1.1 mm | 0.286
5 |  | 1.2 mm | 0.259
6 | Cubic | 0.8 mm | 1.024
7 |  | 0.9 mm | 0.945
8 |  | 1.0 mm | 0.879
9 |  | 1.1 mm | 0.837
10 |  | 1.2 mm | 0.795
11 | Gyroid | 0.8 mm | 0.382
12 |  | 0.9 mm | 0.322
13 |  | 1.0 mm | 0.296
14 |  | 1.1 mm | 0.291
15 |  | 1.2 mm | 0.257

## Slide 2: Prints 2
Layer height (mm) | 0.1
Print speed (mm/s) | 30
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.409
2 |  | 0.9 mm | 0.350
3 |  | 1.0 mm | 0.325
4 |  | 1.1 mm | 0.298
5 |  | 1.2 mm | 0.248
6 | Cubic | 0.8 mm | 1.081
7 |  | 0.9 mm | 1.000
8 |  | 1.0 mm | 0.939
9 |  | 1.1 mm | 0.904
10 |  | 1.2 mm | 0.860
11 | Gyroid | 0.8 mm | 0.399
12 |  | 0.9 mm | 0.335
13 |  | 1.0 mm | 0.308
14 |  | 1.1 mm | 0.301
15 |  | 1.2 mm | 0.259

## Slide 3: Prints 3
Layer height (mm) | 0.1
Print speed (mm/s) | 30
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.372
2 |  | 0.9 mm | 0.332
3 |  | 1.0 mm | 0.308
4 |  | 1.1 mm | 0.292
5 |  | 1.2 mm | 0.289
6 | Cubic | 0.8 mm | 1.107
7 |  | 0.9 mm | 1.019
8 |  | 1.0 mm | 0.949
9 |  | 1.1 mm | 0.909
10 |  | 1.2 mm | 0.851
11 | Gyroid | 0.8 mm | 0.375
12 |  | 0.9 mm | 0.315
13 |  | 1.0 mm | 0.296
14 |  | 1.1 mm | 0.290
15 |  | 1.2 mm | 0.271

## Slide 4: Prints 4
Layer height (mm) | 0.1
Print speed (mm/s) | 35
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.385
2 |  | 0.9 mm | 0.323
3 |  | 1.0 mm | 0.298
4 |  | 1.1 mm | 0.280
5 |  | 1.2 mm | 0.246
6 | Cubic | 0.8 mm | 1.000
7 |  | 0.9 mm | 0.928
8 |  | 1.0 mm | 0.865
9 |  | 1.1 mm | 0.818
10 |  | 1.2 mm | 0.777
11 | Gyroid | 0.8 mm | 0.394
12 |  | 0.9 mm | 0.327
13 |  | 1.0 mm | 0.300
14 |  | 1.1 mm | 0.298
15 |  | 1.2 mm | 0.280
When printed five together, gyroid samples have abnormal trend. It looks like sample 13 has smaller modulus than normal.
I tried to print sample 13 three times and results are stored as Test print 18. Results are not good. Too much variance.
Then I tried to print five gyroid samples one by one, stored as test print 19. I only printed Prints 4 and Prints 5.
The result is still not right. Sample 13 still has abnormal modulus.
Now I try to print five gyroid samples together three times and use average value to represent the true value. Results are stored in test print 20.

## Slide 5: Prints 5
Layer height (mm) | 0.1
Print speed (mm/s) | 35
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.395
2 |  | 0.9 mm | 0.345
3 |  | 1.0 mm | 0.329
4 |  | 1.1 mm | 0.303
5 |  | 1.2 mm | 0.266
6 | Cubic | 0.8 mm | 1.068
7 |  | 0.9 mm | 0.996
8 |  | 1.0 mm | 0.936
9 |  | 1.1 mm | 0.892
10 |  | 1.2 mm | 0.847
11 | Gyroid | 0.8 mm | 0.400
12 |  | 0.9 mm | 0.333
13 |  | 1.0 mm | 0.301
14 |  | 1.1 mm | 0.288
15 |  | 1.2 mm | 0.249

## Slide 6: Prints 6
Layer height (mm) | 0.1
Print speed (mm/s) | 35
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.369
2 |  | 0.9 mm | 0.325
3 |  | 1.0 mm | 0.313
4 |  | 1.1 mm | 0.296
5 |  | 1.2 mm | 0.276
6 | Cubic | 0.8 mm | 1.098
7 |  | 0.9 mm | 1.016
8 |  | 1.0 mm | 0.952
9 |  | 1.1 mm | 0.904
10 |  | 1.2 mm | 0.839
11 | Gyroid | 0.8 mm | 0.394
12 |  | 0.9 mm | 0.327
13 |  | 1.0 mm | 0.298
14 |  | 1.1 mm | 0.296
15 |  | 1.2 mm | 0.276

## Slide 7: Prints 7
Layer height (mm) | 0.1
Print speed (mm/s) | 40
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.381
2 |  | 0.9 mm | 0.328
3 |  | 1.0 mm | 0.298
4 |  | 1.1 mm | 0.285
5 |  | 1.2 mm | 0.254
6 | Cubic | 0.8 mm | 0.988
7 |  | 0.9 mm | 0.915
8 |  | 1.0 mm | 0.847
9 |  | 1.1 mm | 0.806
10 |  | 1.2 mm | 0.767
11 | Gyroid | 0.8 mm | 0.386
12 |  | 0.9 mm | 0.314
13 |  | 1.0 mm | 0.286
14 |  | 1.1 mm | 0.279
15 |  | 1.2 mm | 0.251

## Slide 8: Prints 8
Layer height (mm) | 0.1
Print speed (mm/s) | 40
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.401
2 |  | 0.9 mm | 0.341
3 |  | 1.0 mm | 0.316
4 |  | 1.1 mm | 0.301
5 |  | 1.2 mm | 0.262
6 | Cubic | 0.8 mm | 1.060
7 |  | 0.9 mm | 0.980
8 |  | 1.0 mm | 0.919
9 |  | 1.1 mm | 0.880
10 |  | 1.2 mm | 0.833
11 | Gyroid | 0.8 mm | 0.403
12 |  | 0.9 mm | 0.325
13 |  | 1.0 mm | 0.296
14 |  | 1.1 mm | 0.292
15 |  | 1.2 mm | 0.255

## Slide 9: Prints 9
Layer height (mm) | 0.1
Print speed (mm/s) | 40
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.382
2 |  | 0.9 mm | 0.331
3 |  | 1.0 mm | 0.311
4 |  | 1.1 mm | 0.290
5 |  | 1.2 mm | 0.272
6 | Cubic | 0.8 mm | 1.098
7 |  | 0.9 mm | 1.012
8 |  | 1.0 mm | 0.944
9 |  | 1.1 mm | 0.897
10 |  | 1.2 mm | 0.845
11 | Gyroid | 0.8 mm | 0.404
12 |  | 0.9 mm | 0.325
13 |  | 1.0 mm | 0.298
14 |  | 1.1 mm | 0.296
15 |  | 1.2 mm | 0.269

## Slide 10: Prints 10
Layer height (mm) | 0.1
Print speed (mm/s) | 45
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.376
2 |  | 0.9 mm | 0.316
3 |  | 1.0 mm | 0.290
4 |  | 1.1 mm | 0.278
5 |  | 1.2 mm | 0.254
6 | Cubic | 0.8 mm | 0.959
7 |  | 0.9 mm | 0.883
8 |  | 1.0 mm | 0.818
9 |  | 1.1 mm | 0.778
10 |  | 1.2 mm | 0.737
11 | Gyroid | 0.8 mm | 0.381
12 |  | 0.9 mm | 0.309
13 |  | 1.0 mm | 0.284
14 |  | 1.1 mm | 0.277
15 |  | 1.2 mm | 0.245
Yellow samples were weighted twice, within two days. The weight is consistent.

## Slide 11: Prints 11
Layer height (mm) | 0.1
Print speed (mm/s) | 45
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.408
2 |  | 0.9 mm | 0.342
3 |  | 1.0 mm | 0.318
4 |  | 1.1 mm | 0.301
5 |  | 1.2 mm | 0.255
6 | Cubic | 0.8 mm | 1.060
7 |  | 0.9 mm | 0.987
8 |  | 1.0 mm | 0.924
9 |  | 1.1 mm | 0.883
10 |  | 1.2 mm | 0.836
11 | Gyroid | 0.8 mm | 0.411
12 |  | 0.9 mm | 0.328
13 |  | 1.0 mm | 0.300
14 |  | 1.1 mm | 0.295
15 |  | 1.2 mm | 0.256

## Slide 12: Prints 12
Layer height (mm) | 0.1
Print speed (mm/s) | 45
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.403
2 |  | 0.9 mm | 0.341
3 |  | 1.0 mm | 0.320
4 |  | 1.1 mm | 0.297
5 |  | 1.2 mm | 0.269
6 | Cubic | 0.8 mm | 1.097
7 |  | 0.9 mm | 1.018
8 |  | 1.0 mm | 0.950
9 |  | 1.1 mm | 0.908
10 |  | 1.2 mm | 0.857
11 | Gyroid | 0.8 mm | 0.411
12 |  | 0.9 mm | 0.331
13 |  | 1.0 mm | 0.297
14 |  | 1.1 mm | 0.285
15 |  | 1.2 mm | 0.254

## Slide 13: Prints 13
Layer height (mm) | 0.1
Print speed (mm/s) | 50
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.368
2 |  | 0.9 mm | 0.314
3 |  | 1.0 mm | 0.292
4 |  | 1.1 mm | 0.284
5 |  | 1.2 mm | 0.256
6 | Cubic | 0.8 mm | 0.875
7 |  | 0.9 mm | 0.802
8 |  | 1.0 mm | 0.727
9 |  | 1.1 mm | 0.682
10 |  | 1.2 mm | 0.655
11 | Gyroid | 0.8 mm | 0.376
12 |  | 0.9 mm | 0.304
13 |  | 1.0 mm | 0.284
14 |  | 1.1 mm | 0.279
15 |  | 1.2 mm | 0.250

## Slide 14: Prints 14
Layer height (mm) | 0.1
Print speed (mm/s) | 50
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.409
2 |  | 0.9 mm | 0.344
3 |  | 1.0 mm | 0.319
4 |  | 1.1 mm | 0.305
5 |  | 1.2 mm | 0.260
6 | Cubic | 0.8 mm | 1.050
7 |  | 0.9 mm | 0.979
8 |  | 1.0 mm | 0.915
9 |  | 1.1 mm | 0.874
10 |  | 1.2 mm | 0.823
11 | Gyroid | 0.8 mm | 0.410
12 |  | 0.9 mm | 0.332
13 |  | 1.0 mm | 0.302
14 |  | 1.1 mm | 0.297
15 |  | 1.2 mm | 0.250

## Slide 15: Prints 15
Layer height (mm) | 0.1
Print speed (mm/s) | 50
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.393
2 |  | 0.9 mm | 0.334
3 |  | 1.0 mm | 0.314
4 |  | 1.1 mm | 0.293
5 |  | 1.2 mm | 0.267
6 | Cubic | 0.8 mm | 1.092
7 |  | 0.9 mm | 1.017
8 |  | 1.0 mm | 0.951
9 |  | 1.1 mm | 0.903
10 |  | 1.2 mm | 0.854
11 | Gyroid | 0.8 mm | 0.418
12 |  | 0.9 mm | 0.330
13 |  | 1.0 mm | 0.294
14 |  | 1.1 mm | 0.284
15 |  | 1.2 mm | 0.253

## Slide 16: Prints 16
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 30
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.377
2 |  | 0.9 mm | 0.326
3 |  | 1.0 mm | 0.295
4 |  | 1.1 mm | 0.268
5 |  | 1.2 mm | 0.250
6 | Cubic | 0.8 mm | 0.902
7 |  | 0.9 mm | 0.821
8 |  | 1.0 mm | 0.751
9 |  | 1.1 mm | 0.702
10 |  | 1.2 mm | 0.663
11 | Gyroid | 0.8 mm | 0.367
12 |  | 0.9 mm | 0.314
13 |  | 1.0 mm | 0.275
14 |  | 1.1 mm | 0.272
15 |  | 1.2 mm | 0.253

## Slide 17: Prints 17
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 30
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.404
2 |  | 0.9 mm | 0.341
3 |  | 1.0 mm | 0.320
4 |  | 1.1 mm | 0.300
5 |  | 1.2 mm | 0.268
6 | Cubic | 0.8 mm | 1.070
7 |  | 0.9 mm | 0.987
8 |  | 1.0 mm | 0.917
9 |  | 1.1 mm | 0.879
10 |  | 1.2 mm | 0.847
11 | Gyroid | 0.8 mm | 0.396
12 |  | 0.9 mm | 0.333
13 |  | 1.0 mm | 0.298
14 |  | 1.1 mm | 0.295
15 |  | 1.2 mm | 0.265

## Slide 18: Prints 18
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 30
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.404
2 |  | 0.9 mm | 0.341
3 |  | 1.0 mm | 0.318
4 |  | 1.1 mm | 0.282
5 |  | 1.2 mm | 0.261
6 | Cubic | 0.8 mm | 1.111
7 |  | 0.9 mm | 1.021
8 |  | 1.0 mm | 0.941
9 |  | 1.1 mm | 0.902
10 |  | 1.2 mm | 0.868
11 | Gyroid | 0.8 mm | 0.403
12 |  | 0.9 mm | 0.333
13 |  | 1.0 mm | 0.293
14 |  | 1.1 mm | 0.281
15 |  | 1.2 mm | 0.260

## Slide 19: Prints 19
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 35
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.356
2 |  | 0.9 mm | 0.305
3 |  | 1.0 mm | 0.283
4 |  | 1.1 mm | 0.259
5 |  | 1.2 mm | 0.242
6 | Cubic | 0.8 mm | 0.881
7 |  | 0.9 mm | 0.791
8 |  | 1.0 mm | 0.723
9 |  | 1.1 mm | 0.678
10 |  | 1.2 mm | 0.660
11 | Gyroid | 0.8 mm | 0.367
12 |  | 0.9 mm | 0.307
13 |  | 1.0 mm | 0.276
14 |  | 1.1 mm | 0.270
15 |  | 1.2 mm | 0.253

## Slide 20: Prints 20
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 35
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.402
2 |  | 0.9 mm | 0.333
3 |  | 1.0 mm | 0.316
4 |  | 1.1 mm | 0.292
5 |  | 1.2 mm | 0.263
6 | Cubic | 0.8 mm | 1.069
7 |  | 0.9 mm | 0.987
8 |  | 1.0 mm | 0.923
9 |  | 1.1 mm | 0.880
10 |  | 1.2 mm | 0.840
11 | Gyroid | 0.8 mm | 0.399
12 |  | 0.9 mm | 0.326
13 |  | 1.0 mm | 0.296
14 |  | 1.1 mm | 0.294
15 |  | 1.2 mm | 0.259

## Slide 21: Prints 21
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 35
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.415
2 |  | 0.9 mm | 0.345
3 |  | 1.0 mm | 0.325
4 |  | 1.1 mm | 0.289
5 |  | 1.2 mm | 0.265
6 | Cubic | 0.8 mm | 1.110
7 |  | 0.9 mm | 1.017
8 |  | 1.0 mm | 0.943
9 |  | 1.1 mm | 0.899
10 |  | 1.2 mm | 0.863
11 | Gyroid | 0.8 mm | 0.411
12 |  | 0.9 mm | 0.335
13 |  | 1.0 mm | 0.298
14 |  | 1.1 mm | 0.290
15 |  | 1.2 mm | 0.265

## Slide 22: Prints 22
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 40
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.362
2 |  | 0.9 mm | 0.311
3 |  | 1.0 mm | 0.287
4 |  | 1.1 mm | 0.269
5 |  | 1.2 mm | 0.246
6 | Cubic | 0.8 mm | 0.834
7 |  | 0.9 mm | 0.746
8 |  | 1.0 mm | 0.688
9 |  | 1.1 mm | 0.642
10 |  | 1.2 mm | 0.614
11 | Gyroid | 0.8 mm | 0.364
12 |  | 0.9 mm | 0.299
13 |  | 1.0 mm | 0.268
14 |  | 1.1 mm | 0.267
15 |  | 1.2 mm | 0.251

## Slide 23: Prints 23
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 40
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.401
2 |  | 0.9 mm | 0.340
3 |  | 1.0 mm | 0.319
4 |  | 1.1 mm | 0.298
5 |  | 1.2 mm | 0.264
6 | Cubic | 0.8 mm | 1.054
7 |  | 0.9 mm | 0.970
8 |  | 1.0 mm | 0.909
9 |  | 1.1 mm | 0.865
10 |  | 1.2 mm | 0.813
11 | Gyroid | 0.8 mm | 0.408
12 |  | 0.9 mm | 0.327
13 |  | 1.0 mm | 0.292
14 |  | 1.1 mm | 0.291
15 |  | 1.2 mm | 0.262

## Slide 24: Prints 24
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 40
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.408
2 |  | 0.9 mm | 0.341
3 |  | 1.0 mm | 0.319
4 |  | 1.1 mm | 0.288
5 |  | 1.2 mm | 0.257
6 | Cubic | 0.8 mm | 1.090
7 |  | 0.9 mm | 1.000
8 |  | 1.0 mm | 0.930
9 |  | 1.1 mm | 0.891
10 |  | 1.2 mm | 0.861
11 | Gyroid | 0.8 mm | 0.420
12 |  | 0.9 mm | 0.333
13 |  | 1.0 mm | 0.290
14 |  | 1.1 mm | 0.284
15 |  | 1.2 mm | 0.253

## Slide 25: Prints 25
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 45
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.354
2 |  | 0.9 mm | 0.308
3 |  | 1.0 mm | 0.287
4 |  | 1.1 mm | 0.264
5 |  | 1.2 mm | 0.246
6 | Cubic | 0.8 mm | 0.796
7 |  | 0.9 mm | 0.721
8 |  | 1.0 mm | 0.665
9 |  | 1.1 mm | 0.623
10 |  | 1.2 mm | 0.597
11 | Gyroid | 0.8 mm | 0.365
12 |  | 0.9 mm | 0.294
13 |  | 1.0 mm | 0.265
14 |  | 1.1 mm | 0.265
15 |  | 1.2 mm | 0.24

## Slide 26: Prints 26
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 45
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.403
2 |  | 0.9 mm | 0.336
3 |  | 1.0 mm | 0.314
4 |  | 1.1 mm | 0.293
5 |  | 1.2 mm | 0.257
6 | Cubic | 0.8 mm | 1.033
7 |  | 0.9 mm | 0.958
8 |  | 1.0 mm | 0.892
9 |  | 1.1 mm | 0.848
10 |  | 1.2 mm | 0.794
11 | Gyroid | 0.8 mm | 0.408
12 |  | 0.9 mm | 0.324
13 |  | 1.0 mm | 0.288
14 |  | 1.1 mm | 0.288
15 |  | 1.2 mm | 0.245

## Slide 27: Prints 27
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 45
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.411
2 |  | 0.9 mm | 0.340
3 |  | 1.0 mm | 0.320
4 |  | 1.1 mm | 0.293
5 |  | 1.2 mm | 0.254
6 | Cubic | 0.8 mm | 1.098
7 |  | 0.9 mm | 1.014
8 |  | 1.0 mm | 0.935
9 |  | 1.1 mm | 0.898
10 |  | 1.2 mm | 0.869
11 | Gyroid | 0.8 mm | 0.418
12 |  | 0.9 mm | 0.328
13 |  | 1.0 mm | 0.293
14 |  | 1.1 mm | 0.284
15 |  | 1.2 mm | 0.239

## Slide 28: Prints 28 (might be moist)
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 50
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.340
2 |  | 0.9 mm | 0.290
3 |  | 1.0 mm | 0.271
4 |  | 1.1 mm | 0.248
5 |  | 1.2 mm | 0.232
6 | Cubic | 0.8 mm | 0.761
7 |  | 0.9 mm | 0.689
8 |  | 1.0 mm | 0.629
9 |  | 1.1 mm | 0.590
10 |  | 1.2 mm | 0.568
11 | Gyroid | 0.8 mm | 0.357
12 |  | 0.9 mm | 0.295
13 |  | 1.0 mm | 0.261
14 |  | 1.1 mm | 0.262
15 |  | 1.2 mm | 0.243

## Slide 29: Prints 29
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 50
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.390
2 |  | 0.9 mm | 0.331
3 |  | 1.0 mm | 0.310
4 |  | 1.1 mm | 0.288
5 |  | 1.2 mm | 0.258
6 | Cubic | 0.8 mm | 1.000
7 |  | 0.9 mm | 0.927
8 |  | 1.0 mm | 0.867
9 |  | 1.1 mm | 0.813
10 |  | 1.2 mm | 0.754
11 | Gyroid | 0.8 mm | 0.407
12 |  | 0.9 mm | 0.320
13 |  | 1.0 mm | 0.285
14 |  | 1.1 mm | 0.285
15 |  | 1.2 mm | 0.254

## Slide 30: Prints 30
Layer height (mm) | 0.15 (1st layer 0.1)
Print speed (mm/s) | 50
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.408
2 |  | 0.9 mm | 0.337
3 |  | 1.0 mm | 0.316
4 |  | 1.1 mm | 0.289
5 |  | 1.2 mm | 0.259
6 | Cubic | 0.8 mm | 1.085
7 |  | 0.9 mm | 1.000
8 |  | 1.0 mm | 0.931
9 |  | 1.1 mm | 0.892
10 |  | 1.2 mm | 0.857
11 | Gyroid | 0.8 mm | 0.422
12 |  | 0.9 mm | 0.327
13 |  | 1.0 mm | 0.290
14 |  | 1.1 mm | 0.288
15 |  | 1.2 mm | 0.246

## Slide 31: Prints 31
Layer height (mm) | 0.2
Print speed (mm/s) | 30
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.350
2 |  | 0.9 mm | 0.303
3 |  | 1.0 mm | 0.280
4 |  | 1.1 mm | 0.251
5 |  | 1.2 mm | 0.231
6 | Cubic | 0.8 mm | 0.792
7 |  | 0.9 mm | 0.712
8 |  | 1.0 mm | 0.668
9 |  | 1.1 mm | 0.610
10 |  | 1.2 mm | 0.575
11 | Gyroid | 0.8 mm | 0.352
12 |  | 0.9 mm | 0.293
13 |  | 1.0 mm | 0.261
14 |  | 1.1 mm | 0.261
15 |  | 1.2 mm | 0.243

## Slide 32: Prints 32
Layer height (mm) | 0.2
Print speed (mm/s) | 30
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.397
2 |  | 0.9 mm | 0.338
3 |  | 1.0 mm | 0.314
4 |  | 1.1 mm | 0.284
5 |  | 1.2 mm | 0.266
6 | Cubic | 0.8 mm | 1.051
7 |  | 0.9 mm | 0.967
8 |  | 1.0 mm | 0.893
9 |  | 1.1 mm | 0.855
10 |  | 1.2 mm | 0.817
11 | Gyroid | 0.8 mm | 0.393
12 |  | 0.9 mm | 0.325
13 |  | 1.0 mm | 0.285
14 |  | 1.1 mm | 0.281
15 |  | 1.2 mm | 0.253

## Slide 33: Prints 33
Layer height (mm) | 0.2
Print speed (mm/s) | 30
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.410
2 |  | 0.9 mm | 0.342
3 |  | 1.0 mm | 0.328
4 |  | 1.1 mm | 0.296
5 |  | 1.2 mm | 0.274
6 | Cubic | 0.8 mm | 1.094
7 |  | 0.9 mm | 1.000
8 |  | 1.0 mm | 0.927
9 |  | 1.1 mm | 0.893
10 |  | 1.2 mm | 0.870
11 | Gyroid | 0.8 mm | 0.413
12 |  | 0.9 mm | 0.347
13 |  | 1.0 mm | 0.301
14 |  | 1.1 mm | 0.293
15 |  | 1.2 mm | 0.257

## Slide 34: Prints 34
Layer height (mm) | 0.2
Print speed (mm/s) | 35
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.319
2 |  | 0.9 mm | 0.274
3 |  | 1.0 mm | 0.253
4 |  | 1.1 mm | 0.227
5 |  | 1.2 mm | 0.216
6 | Cubic | 0.8 mm | 0.737
7 |  | 0.9 mm | 0.654
8 |  | 1.0 mm | 0.617
9 |  | 1.1 mm | 0.557
10 |  | 1.2 mm | 0.527
11 | Gyroid | 0.8 mm | 0.310
12 |  | 0.9 mm | 0.255
13 |  | 1.0 mm | 0.222
14 |  | 1.1 mm | 0.222
15 |  | 1.2 mm | 0.203

## Slide 35: Prints 35
Layer height (mm) | 0.2
Print speed (mm/s) | 35
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.391
2 |  | 0.9 mm | 0.333
3 |  | 1.0 mm | 0.313
4 |  | 1.1 mm | 0.283
5 |  | 1.2 mm | 0.257
6 | Cubic | 0.8 mm | 1.023
7 |  | 0.9 mm | 0.936
8 |  | 1.0 mm | 0.878
9 |  | 1.1 mm | 0.837
10 |  | 1.2 mm | 0.785
11 | Gyroid | 0.8 mm | 0.400
12 |  | 0.9 mm | 0.329
13 |  | 1.0 mm | 0.292
14 |  | 1.1 mm | 0.288
15 |  | 1.2 mm | 0.259

## Slide 36: Prints 36
Layer height (mm) | 0.2
Print speed (mm/s) | 35
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.417
2 |  | 0.9 mm | 0.347
3 |  | 1.0 mm | 0.328
4 |  | 1.1 mm | 0.294
5 |  | 1.2 mm | 0.264
6 | Cubic | 0.8 mm | 1.091
7 |  | 0.9 mm | 1.000
8 |  | 1.0 mm | 0.924
9 |  | 1.1 mm | 0.887
10 |  | 1.2 mm | 0.861
11 | Gyroid | 0.8 mm | 0.415
12 |  | 0.9 mm | 0.339
13 |  | 1.0 mm | 0.294
14 |  | 1.1 mm | 0.290
15 |  | 1.2 mm | 0.250

## Slide 37: Prints 37
Layer height (mm) | 0.2
Print speed (mm/s) | 40
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.298
2 |  | 0.9 mm | 0.256
3 |  | 1.0 mm | 0.240
4 |  | 1.1 mm | 0.217
5 |  | 1.2 mm | 0.205
6 | Cubic | 0.8 mm | 0.703
7 |  | 0.9 mm | 0.624
8 |  | 1.0 mm | 0.565
9 |  | 1.1 mm | 0.510
10 |  | 1.2 mm | 0.496
11 | Gyroid | 0.8 mm | 0.289
12 |  | 0.9 mm | 0.232
13 |  | 1.0 mm | 0.205
14 |  | 1.1 mm | 0.205
15 |  | 1.2 mm | 0.186

## Slide 38: Prints 38
Layer height (mm) | 0.2
Print speed (mm/s) | 40
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.390
2 |  | 0.9 mm | 0.329
3 |  | 1.0 mm | 0.313
4 |  | 1.1 mm | 0.285
5 |  | 1.2 mm | 0.259
6 | Cubic | 0.8 mm | 1.017
7 |  | 0.9 mm | 0.937
8 |  | 1.0 mm | 0.874
9 |  | 1.1 mm | 0.831
10 |  | 1.2 mm | 0.774
11 | Gyroid | 0.8 mm | 0.402
12 |  | 0.9 mm | 0.324
13 |  | 1.0 mm | 0.288
14 |  | 1.1 mm | 0.285
15 |  | 1.2 mm | 0.255

## Slide 39: Prints 39
Layer height (mm) | 0.2
Print speed (mm/s) | 40
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.416
2 |  | 0.9 mm | 0.348
3 |  | 1.0 mm | 0.324
4 |  | 1.1 mm | 0.292
5 |  | 1.2 mm | 0.259
6 | Cubic | 0.8 mm | 1.088
7 |  | 0.9 mm | 0.993
8 |  | 1.0 mm | 0.920
9 |  | 1.1 mm | 0.882
10 |  | 1.2 mm | 0.856
11 | Gyroid | 0.8 mm | 0.420
12 |  | 0.9 mm | 0.336
13 |  | 1.0 mm | 0.292
14 |  | 1.1 mm | 0.289
15 |  | 1.2 mm | 0.250

## Slide 40: Prints 40
Layer height (mm) | 0.2
Print speed (mm/s) | 45
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.306
2 |  | 0.9 mm | 0.256
3 |  | 1.0 mm | 0.247
4 |  | 1.1 mm | 0.224
5 |  | 1.2 mm | 0.208
6 | Cubic | 0.8 mm | 0.706
7 |  | 0.9 mm | 0.632
8 |  | 1.0 mm | 0.574
9 |  | 1.1 mm | 0.524
10 |  | 1.2 mm | 0.506
11 | Gyroid | 0.8 mm | 0.334
12 |  | 0.9 mm | 0.263
13 |  | 1.0 mm | 0.234
14 |  | 1.1 mm | 0.236
15 |  | 1.2 mm | 0.217

## Slide 41: Prints 41
Layer height (mm) | 0.2
Print speed (mm/s) | 45
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.395
2 |  | 0.9 mm | 0.331
3 |  | 1.0 mm | 0.313
4 |  | 1.1 mm | 0.286
5 |  | 1.2 mm | 0.258
6 | Cubic | 0.8 mm | 1.011
7 |  | 0.9 mm | 0.933
8 |  | 1.0 mm | 0.865
9 |  | 1.1 mm | 0.823
10 |  | 1.2 mm | 0.761
11 | Gyroid | 0.8 mm | 0.405
12 |  | 0.9 mm | 0.325
13 |  | 1.0 mm | 0.285
14 |  | 1.1 mm | 0.285
15 |  | 1.2 mm | 0.250

## Slide 42: Prints 42
Layer height (mm) | 0.2
Print speed (mm/s) | 45
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.419
2 |  | 0.9 mm | 0.340
3 |  | 1.0 mm | 0.321
4 |  | 1.1 mm | 0.290
5 |  | 1.2 mm | 0.250
6 | Cubic | 0.8 mm | 1.088
7 |  | 0.9 mm | 1.000
8 |  | 1.0 mm | 0.918
9 |  | 1.1 mm | 0.882
10 |  | 1.2 mm | 0.858
11 | Gyroid | 0.8 mm | 0.424
12 |  | 0.9 mm | 0.341
13 |  | 1.0 mm | 0.293
14 |  | 1.1 mm | 0.292
15 |  | 1.2 mm | 0.249

## Slide 43: Prints 43
Layer height (mm) | 0.2
Print speed (mm/s) | 50
Print temperature(℃) | 190
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.303
2 |  | 0.9 mm | 0.258
3 |  | 1.0 mm | 0.244
4 |  | 1.1 mm | 0.220
5 |  | 1.2 mm | 0.203
6 | Cubic | 0.8 mm | 0.666
7 |  | 0.9 mm | 0.584
8 |  | 1.0 mm | 0.537
9 |  | 1.1 mm | 0.490
10 |  | 1.2 mm | 0.470
11 | Gyroid | 0.8 mm | 0.303
12 |  | 0.9 mm | 0.239
13 |  | 1.0 mm | 0.211
14 |  | 1.1 mm | 0.212
15 |  | 1.2 mm | 0.195

## Slide 44: Prints 44
Layer height (mm) | 0.2
Print speed (mm/s) | 50
Print temperature(℃) | 210
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.390
2 |  | 0.9 mm | 0.329
3 |  | 1.0 mm | 0.312
4 |  | 1.1 mm | 0.283
5 |  | 1.2 mm | 0.256
6 | Cubic | 0.8 mm | 0.979
7 |  | 0.9 mm | 0.899
8 |  | 1.0 mm | 0.835
9 |  | 1.1 mm | 0.791
10 |  | 1.2 mm | 0.740
11 | Gyroid | 0.8 mm | 0.415
12 |  | 0.9 mm | 0.330
13 |  | 1.0 mm | 0.285
14 |  | 1.1 mm | 0.281
15 |  | 1.2 mm | 0.248

## Slide 45: Prints 45
Layer height (mm) | 0.2
Print speed (mm/s) | 50
Print temperature(℃) | 230
Index | Infill pattern | Line distance | Weight (g)
1 | Line | 0.8 mm | 0.411
2 |  | 0.9 mm | 0.340
3 |  | 1.0 mm | 0.323
4 |  | 1.1 mm | 0.292
5 |  | 1.2 mm | 0.259
6 | Cubic | 0.8 mm | 1.084
7 |  | 0.9 mm | 0.992
8 |  | 1.0 mm | 0.915
9 |  | 1.1 mm | 0.878
10 |  | 1.2 mm | 0.847
11 | Gyroid | 0.8 mm | 0.428
12 |  | 0.9 mm | 0.341
13 |  | 1.0 mm | 0.290
14 |  | 1.1 mm | 0.292
15 |  | 1.2 mm | 0.244

## Slide 46: DOE
Parameters | Levels
Layer height (mm) | 0.1, 0.15, 0.2
Line distance (mm) | 0.8, 0.9, 1.1, 1.0, 1.2
Infill pattern | Lines, Cubic, Gyroid
Print speed (mm/s) | 30, 35, 40, 45, 50
Print temperature(℃) | 190, 210, 230
DOE (total samples: 675)
0.25 mm nozzle.
No top/bottom layers, no walls, no “Connect infill lines”.
Travel speed 50 mm/s.
First layer height same as other layers.